|  |  | ###### OESTE AISLANTE ###### www.oesteaislante.com.ar ventas@oesteaislante.com.ar |  |  |  |  | - Fundada en 1949 - Cuit: 30-58576670-0 - Ing.Brutos: 0466669-11 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | TECHNICAL SPECIFICATION SHEET (J-200) |  |  |  |  |  |  |  |  |  |
|  | DESCRIPTION: J-200 grade film is a transparent and untreated bi-axially oriented polyester film; film complies with FDA and EC regulations. APPLICATIONS: Suitable for printing, lamination & metallization. SALIENT FEATURES: - Good clarity - Good Adhesion to inks - Excellent Machinability - Excellent Mechanical and Thermal Properties - Excellent for printing and lamination |  |  |  |  |  |  |  |  |  |
|  | TECHNICAL DATA |  |  |  |  |  |  |  |  |  |
|  | Properties |  |  | Test method | Unit | J-200 |  |  |  |  |
|  | PHYSICAL |  |  |  |  |  |  |  |  |  |
|  | Thickness |  |  | ASTM D-374 | Micron (Gauge) | 10 (40) |  | 12 (48) | 15 (60) |  |
|  | Yield |  |  | MTM | m2/kg (in2 /lb) | 71.4 (50200) |  | 59.5 (41800) | 47.6 (33500) |  |
|  | OPTICAL |  |  |  |  |  |  |  |  |  |
|  | Haze |  |  | ASTM D-1003 | % | 3.5 |  | 3.5 | 3.5 |  |
|  | Total luminous transmittance |  |  | ASTM D-1003 | % | 89 |  | 89 | 89 |  |
|  | MECHANICAL |  |  |  |  |  |  |  |  |  |
|  | Tensile Strength (Min) |  | MD | ASTM D-882 | Kg/cm2 (psi) | 2000 (28500) |  | 2000 (28500) | 2000 (28500) |  |
|  |  |  | TD | ASTM D-882 | Kg/cm2 (psi) | 1900 (27000) |  | 1900 (27000) | 1900 (27000) |  |
|  | Elongation (Min) |  | MD | ASTM D-882 | % | 90 |  | 90 | 90 |  |
|  |  |  | TD | ASTM D-882 | % | 90 |  | 90 | 90 |  |
|  | Coefficient of friccion (Side-A / B) (Max) |  | St | ASTM D-1894 | - | 0.50 |  | 0.50 | 0.50 |  |
|  |  |  | Dy | ASTM D-1894 | - | 0.45 |  | 0.45 | 0.45 |  |
|  | THERMAL |  |  |  |  |  |  |  |  |  |
|  | Shrinkage (Max) (150ºC / 30 min) |  | MD | ASTM D-1204 | % | 2.80 |  | 2.80 | 2.80 |  |
|  |  |  | TD | ASTM D-1204 | % | 0.40 |  | 0.40 | 0.40 |  |
|  | SURFACE |  |  |  |  |  |  |  |  |  |
|  | Wetting tension (Min) |  |  | ASTM D-2578 | Dyne / cm | 44 |  | 44 | 44 |  |
|  | BARRIER |  |  |  |  |  |  |  |  |  |
|  | W.V.T.R (38ºC & 90% RH) (Max) |  |  | ASTM E-398 | g / m2 / day (g / 100 inch2 / day) | 55 (3.6) |  | 45 (3.0) | 38 (2.5) |  |
|  | O.T.R (23ºC & 0% RH) (Max) |  |  | ASTM D-3985 | cc / m2 / day (cc / 100 inch2 / day) | 130 (8.5) |  | 110 (7.0) | 90 (5.8) |  |
|  | The values given in this technical datasheet are typical performance data and are believed to be accurate. These are given in good faith but it is for the customer to satisfy of the suitability for its own particular purpose. MANUFACTURER suggests the customer to confirm these values and product compatibility prior to their use and the company offers neither guarantee nor accepts any responsability for the fitness of the product for any particular use. |  |  |  |  |  |  |  |  |  |
|  | MTM: MANUFACTURER TEST METHOD, MD: MACHINE DIRECTION, TD: TRANSVERSE DIRECTION |  |  |  |  |  |  |  |  |  |
|  | - Virgilio 280 (C1407BQD) Buenos Aires – Argentina (54 11) 4683-1632 /2906 /4064 fax |  |  |  |  |  |  |  |  |  |

|  |  | ###### OESTE AISLANTE ###### www.oesteaislante.com.ar ventas@oesteaislante.com.ar |  |  |  |  | - Fundada en 1949 - Cuit: 30-58576670-0 - Ing.Brutos: 0466669-11 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | TECHNICAL SPECIFICATION SHEET (J-200) |  |  |  |  |  |  |  |  |  |
|  | DESCRIPTION: J-200 grade film is a transparent and untreated bi-axially oriented polyester film; film complies with FDA and EC regulations. APPLICATIONS: Suitable for pinting, lamination & metallization. SALIENT FEATURES: - Good clarity - Good Adhesion to inks - Excellent Machinability - Excellent Mechanical and Thermal Properties - Excellent for printing and lamination |  |  |  |  |  |  |  |  |  |
|  | TECHNICAL DATA |  |  |  |  |  |  |  |  |  |
|  | Properties |  |  | Test method | Unit | J-200 |  |  |  |  |
|  | PHYSICAL |  |  |  |  |  |  |  |  |  |
|  | Thickness |  |  | ASTM D-374 | Micron (Gauge) | 23 (92) |  | 36 (144) | 50 (200) |  |
|  | Yield |  |  | MTM | m2/kg (in2 /lb) | 31 (21800) |  | 19.8 (13900) | 14 (10000) |  |
|  | OPTICAL |  |  |  |  |  |  |  |  |  |
|  | Haze |  |  | ASTM D-1003 | % | 4.0 |  | 4.0 | 4.0 |  |
|  | Total luminous transmittance |  |  | ASTM D-1003 | % | 89 |  | 89 | 89 |  |
|  | MECHANICAL |  |  |  |  |  |  |  |  |  |
|  | Tensile Strength (Min) |  | MD | ASTM D-882 | Kg/cm2 (psi) | 2000 (28500) |  | 1900 (27000) | 1900 (27000) |  |
|  |  |  | TD | ASTM D-882 | Kg/cm2 (psi) | 1900 (27000) |  | 1800 (25600) | 1800 (25600) |  |
|  | Elongation (Min) |  | MD | ASTM D-882 | % | 90 |  | 100 | 100 |  |
|  |  |  | TD | ASTM D-882 | % | 90 |  | 90 | 90 |  |
|  | Coefficient of friccion (Side-A / B) (Max) |  | St | ASTM D-1894 | - | 0.50 |  | 0.50 | 0.50 |  |
|  |  |  | Dy | ASTM D-1894 | - | 0.45 |  | 0.45 | 0.45 |  |
|  | THERMAL |  |  |  |  |  |  |  |  |  |
|  | Shrinkage (Max) (150ºC / 30 min) |  | MD | ASTM D-1204 | % | 2.80 |  | 2.80 | 2.80 |  |
|  |  |  | TD | ASTM D-1204 | % | 0.40 |  | 0.40 | 0.40 |  |
|  | SURFACE |  |  |  |  |  |  |  |  |  |
|  | Wetting tension (Min) |  |  | ASTM D-2578 | Dyne / cm | 44 |  | 44 | 44 |  |
|  | BARRIER |  |  |  |  |  |  |  |  |  |
|  | WVTR (38ºC & 90% RH) (Max) |  |  | ASTM E-398 | g / m2 / day (g / 100 inch2 / day) | 28 (1.8) |  | 22 (1.4) | 18 (1.2) |  |
|  | OTR (23ºC & 0% RH) (Max) |  |  | ASTM D-3985 | cc / m2 / day (cc / 100 inch2 / day) | 70 (4.5) |  | 50 (3.2) | 30 (2.0) |  |
|  | The values given in this technical datasheet are typical performance data and are believed to be accurate. These are given in good faith but it is for the customer to satisfy of the suitability for its own particular purpose. MANUFACTURER suggests the customer to confirm these values and product compatibility prior to their use and the company offers neither guarantee nor accepts any responsability for the fitness of the product for any particular use. |  |  |  |  |  |  |  |  |  |
|  | MTM: MANUFACTURER TEST METHOD, MD: MACHINE DIRECTION, TD: TRANSVERSE DIRECTION |  |  |  |  |  |  |  |  |  |
|  | - Virgilio 280 (C1407BQD) Buenos Aires – Argentina (54 11) 4683-1632 /2906 /4064 fax |  |  |  |  |  |  |  |  |  |