|  |  | ###### OESTE AISLANTE ###### www.oesteaislante.com.ar ventas@oesteaislante.com.ar |  |  |  |  |  |  |  | - Fundada en 1949 - Cuit: 30-58576670-0 - Ing.Brutos: 0466669-11 |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | TECHNICAL SPECIFICATION SHEET (J-470) |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | DESCRIPTION: J-470 is co extruded tough milky white film having excellent surface and good handling property APPLICATIONS: Suitable insulation in rotating electrical machine and other general purpose application. SALIENT FEATURES: - Tough flexibility to prevent delamination - Good insulation property - Excellent Machinability - Excellent Mechanical Properties - Excellent Dimensional Stability |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | TECHNICAL DATA |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Properties |  |  |  | Test method |  | Unit |  | J-470 |  |  |  |  |  |
|  | PHYSICAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Thickness |  |  |  | ASTM D-374 |  | Micron (Gauge) |  | 100 (400) |  |  | 125 (500) | 190 (760) |  |
|  | Yield |  |  |  | MTM |  | m2/kg (in2 /lb) |  | 7.1 (4990) |  |  | 5.7 (4000) | 3.7 (2600) |  |
|  | OPTICAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Haze |  |  |  | ASTM D-1003 |  | % |  | 65 |  |  | 70 | 80 |  |
|  | Total luminous transmittance |  |  |  | ASTM D-1003 |  | % |  | 80 |  |  | 75 | 71 |  |
|  | MECHANICAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Tensile Strength (Min) |  | MD |  | ASTM D-882 |  | Kg/cm2 (psi) |  | 1700 (24200) |  |  | 1700 (24200) | 1700 (24200) |  |
|  |  |  | TD |  | ASTM D-882 |  | Kg/cm2 (psi) |  | 1700 (24200) |  |  | 1700 (24200) | 1700 (24200) |  |
|  | Elongation (Min) |  | MD |  | ASTM D-882 |  | % |  | 120 |  |  | 120 | 120 |  |
|  |  |  | TD |  | ASTM D-882 |  | % |  | 100 |  |  | 100 | 100 |  |
|  | Coefficient of friccion (Side-A / B) (Max) |  | St |  | ASTM D-1894 |  | - |  | 0.35 |  |  | 0.35 | 0.35 |  |
|  |  |  | Dy |  | ASTM D-1894 |  | - |  | 0.30 |  |  | 0.30 | 0.30 |  |
|  | THERMAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Shrinkage (Max) (150ºC / 30 min) |  | MD |  | ASTM D-1204 |  | % |  | 2.50 |  |  | 2.50 | 2.50 |  |
|  |  |  | TD |  | ASTM D-1204 |  | % |  | 1.50 |  |  | 1.50 | 1.50 |  |
|  | ELECTRICAL |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Break Down Voltage |  |  | ASTM D-149 |  | KV/inch |  | 15 |  |  | 17 |  | 20 |  |
|  | Volume Resistivity |  |  | ASTM D-256 |  | Ohm cm |  | 10^16 |  |  | 10^16 |  | 10^16 |  |
|  | The values given in this technical datasheet are typical performance data and are believed to be accurate. These are given in good faith but it is for the customer to satisfy of the suitability for its own particular purpose. MANUFACTURER suggests the customer to confirm these values and product compatibility prior to their use and the company offers neither guarantee nor accepts any responsability for the fitness of the product for any particular use. |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | MTM: MANUFACTURER TEST METHOD, MD: MACHINE DIRECTION, TD: TRANSVERSE DIRECTION |  |  |  |  |  |  |  |  |  |  |  |  |  |
|  | - Virgilio 280 (C1407BQD) Buenos Aires – Argentina (54 11) 4683-1632 /2906 /4064 fax |  |  |  |  |  |  |  |  |  |  |  |  |  |

|  |  | ###### OESTE AISLANTE ###### www.oesteaislante.com.ar ventas@oesteaislante.com.ar |  |  |  |  |  |  |  | - Fundada en 1949 - Cuit: 30-58576670-0 - Ing.Brutos: 0466669-11 |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- | --- |
|  | TECHNICAL SPECIFICATION SHEET (J-470) |  |  |  |  |  |  |  |  |  |  |  |  |
|  | DESCRIPTION: J-470 is co extruded tough milky white film having excellent surface and good handling property APPLICATIONS: Suitable insulation in rotating electrical machine and other general purpose application. SALIENT FEATURES: - Tough flexibility to prevent delamination - Goog insulation property - Excellent Machinability - Excellent Mechanical Properties - Excellent Dimensional Stability |  |  |  |  |  |  |  |  |  |  |  |  |
|  | TECHNICAL DATA |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Properties |  |  |  | Test method |  | Unit |  | J-470 |  |  |  |  |
|  | PHYSICAL |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Thickness |  |  |  | ASTM D-374 |  | Micron (Gauge) |  | 250 (1000) |  |  | 350 (1400) |  |
|  | Yield |  |  |  | MTM |  | m2/kg (in2 /lb) |  | 2.9 (2040) |  |  | 2.1 (1440) |  |
|  | OPTICAL |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Haze |  |  |  | ASTM D-1003 |  | % |  | 90 |  |  | 100 |  |
|  | Total luminous transmittance |  |  |  | ASTM D-1003 |  | % |  | 67 |  |  | 63 |  |
|  | MECHANICAL |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Tensile Strength (Min) |  | MD |  | ASTM D-882 |  | Kg/cm2 (psi) |  | 1600 (28800) |  |  | 1600 (28800) |  |
|  |  |  | TD |  | ASTM D-882 |  | Kg/cm2 (psi) |  | 1600 (28800) |  |  | 1600 (28800) |  |
|  | Elongation (Min) |  | MD |  | ASTM D-882 |  | % |  | 140 |  |  | 150 |  |
|  |  |  | TD |  | ASTM D-882 |  | % |  | 120 |  |  | 130 |  |
|  | Coefficient of friccion (Side-A / B) (Max) |  | St |  | ASTM D-1894 |  | - |  | 0.35 |  |  | 0.35 |  |
|  |  |  | Dy |  | ASTM D-1894 |  | - |  | 0.30 |  |  | 0.30 |  |
|  | THERMAL |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Shrinkage (Max) (150ºC / 30 min) |  | MD |  | ASTM D-1204 |  | % |  | 2.5 |  |  | 2.5 |  |
|  |  |  | TD |  | ASTM D-1204 |  | % |  | 1.5 |  |  | 1.5 |  |
|  | ELECTRICAL |  |  |  |  |  |  |  |  |  |  |  |  |
|  | Break Down Voltage |  |  | ASTM D-149 |  | KV/inch |  | 22 |  |  | 26 |  |  |
|  | Volume Resistivity |  |  | ASTM D-256 |  | Ohm cm |  | 10^16 |  |  | 10^16 |  |  |
|  | The values given in this technical datasheet are typical performance data and are believed to be accurate. These are given in good faith but it is for the customer to satisfy of the suitability for its own particular purpose. MANUFACTURER suggests the customer to confirm these values and product compatibility prior to their use and the company offers neither guarantee nor accepts any responsability for the fitness of the product for any particular use. |  |  |  |  |  |  |  |  |  |  |  |  |
|  | MTM: MANUFACTURER TEST METHOD, MD: MACHINE DIRECTION, TD: TRANSVERSE DIRECTION |  |  |  |  |  |  |  |  |  |  |  |  |
|  | - Virgilio 280 (C1407BQD) Buenos Aires – Argentina (54 11) 4683-1632 /2906 /4064 fax |  |  |  |  |  |  |  |  |  |  |  |  |