TECHNICAL SPECIFICATION SHEET (J-530)

DESCRIPTION: J-530 is untreated, Co extruded standard clear film having excellent surface, good clarity, superior gloss and good handling property

APPLICATIONS: High clarity film suitable for Metallization, holographic, high quality lamination and other general purpose application.

SALIENT FEATURES:

- High clarity and Transparency

- High surface gloss

- Excellent Machinability

- Excellent Mechanical Properties

- Excellent Dimensional Stability

| TECHNICAL DATA |  |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- | --- |
| Properties |  | Test method | Unit | J-530 |  |  |  |
| PHYSICAL |  |  |  |  |  |  |  |
| Thickness |  | ASTM D-374 | Micron (Gauge) | 75 (300) | 100 (400) | 125 (500) | 150 (600) |
| Yield |  | MTM | m2/kg (in2 /lb) | 9.5 (6680) | 7.1 (4990) | 5.7 (4000) | 4.7 (3300) |
| OPTICAL |  |  |  |  |  |  |  |
| Haze |  | ASTM D-1003 | % | 2.0 | 2.2 | 2.5 | 2.7 |
| Total luminous transmittance |  | ASTM D-1003 | % | 89 | 89 | 89 | 89 |
| MECHANICAL |  |  |  |  |  |  |  |
| Tensile Strength (Min) | MD | ASTM D-882 | Kg/cm2 (psi) | 1700 (24200) | 1700 (24200) | 1700 (24200) | 1700 (24200) |
|  | TD | ASTM D-882 | Kg/cm2 (psi) | 1700 (24200) | 1700 (24200) | 1700 (24200) | 1700 (24200) |
| Elongation (Min) | MD | ASTM D-882 | % | 120 | 120 | 120 | 120 |
|  | TD | ASTM D-882 | % | 100 | 100 | 100 | 100 |
| Coefficient of friccion (Side-A / B) (Max) | St | ASTM D-1894 | - | 0.45 | 0.45 | 0.45 | 0.45 |
|  | Dy | ASTM D-1894 | - | 0.35 | 0.35 | 0.35 | 0.35 |
| THERMAL |  |  |  |  |  |  |  |
| Shrinkage (Max) (150ºC / 30 min) | MD | ASTM D-1204 | % | 2.5 | 2.5 | 2.5 | 2.5 |
|  | TD | ASTM D-1204 | % | 1.5 | 1.5 | 1.5 | 1.5 |
| SURFACE |  |  |  |  |  |  |  |
| Wetting tension (Min) |  | ASTM D-2578 | Dyne / cm | 44 | 44 | 44 | 44 |
| ELECTRICAL |  |  |  |  |  |  |  |
| Volume Resistivity |  | ASTM D-256 | Ohm cm | 10^16 | 10^16 | 10^16 | 10^16 |

MTM: MANUFACTURER TEST METHOD, MD: MACHINE DIRECTION, TD: TRANSVERSE DIRECTION

The values given in this technical datasheet are typical performance data and are believed to be accurate. These are given in good faith but it is for the customer to satisfy of the suitability for its own particular purpose. MANUFACTURER suggests the customer to confirm these values and product compatibility prior to their use and the company offers neither guarantee nor accepts any responsability for the fitness of the product for any particular use.

TECHNICAL SPECIFICATION SHEET (J-530)

DESCRIPTION: J-530 is untreated, Co extruded standard clear film having excellent surface, good clarity, superior gloss and good handling property

APPLICATIONS: High clarity film suitable for Metallization, holographic, high quality lamination and other general purpose application.

SALIENT FEATURES:

- High clarity and Transparency

- High surface gloss

- Excellent Machinability

- Excellent Mechanical Properties

- Excellent Dimensional Stability

| TECHNICAL DATA |  |  |  |  |  |  |
| --- | --- | --- | --- | --- | --- | --- |
| Properties |  | Test method | Unit | J-530 |  |  |
| PHYSICAL |  |  |  |  |  |  |
| Thickness |  | ASTM D-374 | Micron (Gauge) | 175 (700) | 188 (752) | 250 (1000) |
| Yield |  | MTM | m2/kg (in2 /lb) | 4.1 (2880) | 3.8 (2650) | 2.9 (2040) |
| OPTICAL |  |  |  |  |  |  |
| Haze |  | ASTM D-1003 | % | 3.0 | 3.5 | 4.5 |
| Total luminous transmittance |  | ASTM D-1003 | % | 89 | 89 | 89 |
| MECHANICAL |  |  |  |  |  |  |
| Tensile Strength (Min) | MD | ASTM D-882 | Kg/cm2 (psi) | 1700 (24200) | 1650 (23500) | 1600 (22800) |
|  | TD | ASTM D-882 | Kg/cm2 (psi) | 1700 (24200) | 1650 (23500) | 1600 (22800) |
| Elongation (Min) | MD | ASTM D-882 | % | 120 | 120 | 120 |
|  | TD | ASTM D-882 | % | 100 | 100 | 100 |
| Coefficient of friccion (Side-A / B) (Max) | St | ASTM D-1894 | - | 0.45 | 0.45 | 0.45 |
|  | Dy | ASTM D-1894 | - | 0.35 | 0.35 | 0.35 |
| THERMAL |  |  |  |  |  |  |
| Shrinkage (Max) (150ºC / 30 min) | MD | ASTM D-1204 | % | 2.5 | 2.5 | 2.5 |
|  | TD | ASTM D-1204 | % | 1.5 | 1.5 | 1.5 |
| SURFACE |  |  |  |  |  |  |
| Wetting tension (Min) |  | ASTM D-2578 | Dyne / cm | 44 | 44 | 44 |
| ELECTRICAL |  |  |  |  |  |  |
| Volume Resistivity |  | ASTM D-256 | Ohm cm | 10^16 | 10^16 | 10^16 |

MTM: MANUFACTURER TEST METHOD, MD: MACHINE DIRECTION, TD: TRANSVERSE DIRECTION

The values given in this technical datasheet are typical performance data and are believed to be accurate. These are given in good faith but it is for the customer to satisfy of the suitability for its own particular purpose. MANUFACTURER suggests the customer to confirm these values and product compatibility prior to their use and the company offers neither guarantee nor accepts any responsability for the fitness of the product for any particular use.